Пример отчета

NOVA instruments

©1994-2007, Quantachrome Instruments version 9.0

Analysis                                          Report

Operator: Ditts                            Date:2008/07/08     Operator: Ditts               Date:7/23/2008

Sample ID:  Al50-50                Filename:      C:\QCdata\Physisorb\Al50-50_0080708_1.qps

Sample Desc:                            Comment:       Al50-50

Sample weight: 0.3433 g          Sample Volume: 0.05572 cc

Outgas Time:   6.0 hrs              OutgasTemp:    150.0 C

Analysis gas:  Nitrogen            Bath Temp:     77.3 K

Press. Tolerance:0.100/0.100 (ads/des)Equil time: 60/60 sec (ads/des) Equil timeout: 240/240 sec (ads/des)

Analysis Time: 20.9 min            End of run:    2008/07/08 3:09:47  Instrument:    Nova Station A

Cell ID:        66

Adsorbate      Nitrogen                 Temperature    77.350K

Molec. Wt.: 28.013  g    Cross Section: 16.200  Å²     Liquid Density: 0.808  g/cc

Relative|Pressure                 Volume @ STP                1 / [ W((Po/P) - 1) ]

P/Po                            cc/g

4.57600e-02                     0.4937                          7.7723e+01

1.69358e-01                     0.8027                          2.0322e+02

2.34503e-01                     0.9177                          2.6707e+02

2.96071e-01                     1.0162                          3.3117e+02

3.52285e-01                     1.0932                          3.9807e+02

BET summary

Slope =      1035.236

Intercept =         2.812e+01

Correlation coefficient, r =         0.999512

C constant=        37.814

Surface Area =         3.275 m²/g