|  | Acoustic Emission Testing (AE) |
| --- | --- |
|  | Acoustic Impedance (Z) |
|  | Acoustic Properties |
|  | Ampere |
|  | Amplifier |
|  | Amplitude |
|  | Attenuation |
|  | Background fluorescence |
|  | Calibration |
|  | Capillary Action |
|  | Coil |
|  | Collimator |
|  | Conductivity |
|  | Crack |
|  | Cyclic Load |
|  | Decibel |
|  | Defect |
|  | Densitometer |
|  | Developer (Penetrant) |
|  | Diamagnetic Materials |
|  | Dry Developer |
|  | Dwell Time |
|  | Eddy Currents |
|  | Eddy Current Inspection |
|  | Electromagnetic Radiation |
|  | Fatigue Cracks |
|  | Ferromagnetic Materials |
|  | Fluorescent |
|  | Fracture |
|  | Fracture Mechanics |
|  | Frequency |
|  | Gas Holes |
|  | Half-life |
|  | Induction |
|  | Insulators |
|  | Leak Testing |
|  | Liquid Penetrant Inspection |
|  | Magnetic Particle Inspection |
|  | Nondestructive Evaluation |
|  | Nondestructive Testing |
|  | Penetrant |
|  | Penetrant Testing |
|  | Piezoelectric Transducers |
|  | Radiography |
|  | Refraction |
|  | Scanning |
|  | Sensitivity |
|  | Sensitivity Panel |
|  | Sound |
|  | Suspension |
|  | Ultrasonic |
|  | Ultrasonic Testing |
|  | Vibration |
|  | Visible dye penetrant |
|  | Weld Crack |
|  | X-ray Sources |

|  | A break, or separation, of a part into two or more pieces. |
| --- | --- |
|  | A bright vivid color that glows under a black light. |
|  | A crack in weld metal. |
|  | A device for limiting the effects of beam spread. |
|  | A device to increase or amplify electric impulses. |
|  | A discontinuity or other imperfection causing a reduction in the quality of a material or component. |
|  | A finely divided powder applied over the surface of a part to help bring out penetrant indications. |
|  | A fluid (usually a liquid but can be a gas) which possesses unique properties that render it highly capable of entering small openings, a characteristic which makes this fluid especially suitable for use in the detection of surface discontinuities which may be present. |
|  | A logarithmic unit for expressing power relationships. n = 10 log10(I1/I2) where n is the difference of decibels of intensities 1 & 2. |
|  | A long narrow discontinuity |
|  | A measure of the ability of a material to conduct electrical current. |
|  | A measure of the ability to detect small signals. Limited by the signal-to-noise ratio. |
|  | A method of detecting cracks or defects by establishing a magnetic field in the object and using iron filings to see if the field lines are constant. |
|  | A method that is used to reveal surface breaking flaws by bleedout of a colored or fluorescent dye from the flaw. |
|  | A nondestructive testing method that "listens" for transient elastic-waves generated due to a rapid release of strain energy caused by a structural alteration in a solid material. |
|  | A plated metal panel with cracks of know depth induced into the plating; used to evaluate and compare penetrant sensitivity. |
|  | A powder that is applied dry to the test component when performing a penetrant inspection. |
|  | A quantitative analysis for evaluating structural behavior in terms of applied stress, crack length, and specimen or machine component geometry. |
|  | A rapid back and forth motion of a particle or solid. |
|  | A standard unit of measure for electric current or the flow of electrons. The amount of current sent by one volt through a resistance of one ohm. |
|  | A term referring to acoustic vibration frequencies greater than about 20,000 hertz. |
|  | A tool that takes an electrical signal and turns it into mechanical vibrations, or takes vibrations and turns it into an electrical signal. |
|  | An electromagnetic technique used on conductive materials for crack detection or the rapid sorting of small components for either flaws, size variations, or material variation, as well as other applications. |
|  | An instrument used to measure the degree of darkening of developed radiographic film. |
|  | An intensely colored (usually red) highly penetrating liquid which will provide maximum contrast with the white developer when used for detection of surface discontinuities. |
|  | An object that produces x-rays. |
|  | Circular induced currents that are generated by an alternating current in the nearby coil. |
|  | Cracks in a material formed from repeated stress, none of which exceeded the maximum stress of the material. |
|  | Energy in a wave form that possesses both electrical and magnetic characteristics. |
|  | Fluorescent residues observed over the general surface of the part during fluorescent penetrant inspection. |
|  | Holes created by a gas escaping from molten metal. |
|  | Intrinsic characteristics of any particular material that describe how sound travels through it. Such characteristics include the density, acoustic impedance, and sound velocity |
|  | Liquid bath in which a solid is suspended in liquid. |
|  | Materials that can be magnetized. |
|  | Materials that have all paired electrons in the atoms and thus have no net magnetic moment. The magnetic permeability is usually very close to 1. |
|  | Materials that resist the flow of electrons. |
|  | Mechanical vibrations transmitted by an elastic medium. |
|  | Method that is used to reveal surface breaking flaws by bleedout of a colored or fluorescent dye from the flaw. |
|  | More than one loop of a conductor wound in a spiral. Also called a solenoid. |
|  | Movement of the transducer over the surface of the test object in a controlled manner so as to achieve complete coverage. |
|  | Repetitive loading of a material that sometimes leads to fatigue fracture. |
|  | Techniques are used to detect and locate leaks in pressure containment parts, pressure vessels, and structures. |
|  | Testing to detect defects in materials using techniques that do not damage or destroy the items being tested. |
|  | The amount of time it takes for half of the atoms in a given mass to decay. |
|  | The change in direction of an acoustic wave as the ultrasonic beam passes from one medium into another having a different sound velocity. |
|  | The maximum absolute value obtained by the disturbance of a wave or any quantity that varies periodically |
|  | The number of waves that pass a given point in a specified unit of time. |
|  | The period of time wherein penetrant or developer is in contact with the surface of the part. Drain time is considered to be a portion of the dwell time. Synonymous with penetration time or emulsifier time. |
|  | The phenomenon of a liquid such as water spontaneously creeping up thin tubes and fibers, this is caused by adhesive and cohesive forces and surface tension. |
|  | The process of generating current in a conductor by placing the conductor in a changing magnetic field. |
|  | The process of making a radiograph |
|  | The process whereby the magnitude of the output of a measuring instrument is related to the magnitude of the input force driving the instrument. |
|  | The reduction in the level of a quantity, such as the intensity of a wave or radiation. |
|  | The resistance of a material to the passage of sound waves. |
|  | The transmission of high-frequency sound waves into a material to detect imperfections or to locate changes in material properties. |
|  | The use of non-invasive techniques to determine the integrity of a material, component or structure, or to quantitatively measure some characteristic of an object. |