Nondestructive Testing 
International Normative Technical Documentation

Course Overview

| Level of study | Master Degree |
| --- | --- |
| Workload | ECTS: количество кредитов Total Hours: Contact Hours: 32 · Lectures: 12 · Labs: 20 · Seminars: - |
| Course Code | none |
| Semester | Summer 2 |
| Prerequisites | Physics, metrology and technical measurements |
| Course Objectives | · Forming of theoretical knowledge on nondestructive testing methods · Acquiring practical skills on the technology of different nondestructive testing methods |
| Learning Outcomes | After completing the course, a student should know: · physical and physiological fundamentals of NDT methods; · basic devices and instruments of NDT methods; · techniques of NDT methods; · standards and other normative documents on NDT methods; · safety requirements. |
| Syllabus | · Visual Testing, · Liquid Penetrant Testing, · Electromagnetic Testing, · Ultrasonic Testing, · Thermal/Infrared Testing, · Radiographic Testing. |
| Labs | · Visual and measuring testing of the welds · Technological process of Liquid Penetrant Testing. Color method. · General introduction to X-ray. Full processing cycle and analysis of the image. · General introduction to ultrasonic defectoscopes. · Electromagnetic Testing: Measurement of thickness, Measurement of electrical conductivity, Eddy current flaw detector, Magnetic particle testing, Electric control. · Thermal/Infrared Testing using a thermal imager. |
| Projects | none |
| Assessment | · Intermediate control by means of tests · Final Credit Test ( Pass/Fail) |
| Resources | · Charles J. H., “Hand Book of Nondestructive Testing”, MsGraw-Hill, Madrid, 2003 · http://www.efndt.org/ – The European Federation for NDT · http://www.icndt.org/ – The International Committee for Non-Destructive Testing · http://www.izfp.fraunhofer.de – The Fraunhofer Institute for Nondestructive Testing · https://www.asnt.org/ – American Society for Nondestructive Testing · https://www.asme.org/ – American Society of Mechanical Engineers |
| Instructors | Kalinichenko Alexey http://portal.tpu.ru:7777/SHARED/l/LEX-K/eng/ |